## Slide 1
MAGNITO · COMPUTATIONAL SCREENING
Fe-rich Heavy-Rare-Earth
Magnet Search
Search criteria, database landscape, the ferro- vs ferrimagnetic test, and an active-learning path forward
Target: μ₀Ms > 2 T · Tc > 550 K · uniaxial anisotropy · RE-lean
706 paired DFT calculations · 353 compounds · 180 credible RE-TM exchange labels · 0 ferromagnets
Fe / Co
↑
↑
↑
↑
Gd / Tb / Dy / Ho / Er / Tm
↓
4f moment antiparallel
→ ferrimagnet, not ferromagnet
Notes: Framing: the program wants >2 T. The physics obstacle is that heavy-RE 4f moments couple antiparallel to Fe, so the default outcome is a ferrimagnet with a reduced net moment.

## Slide 2
WHY THIS SEARCH IS HARD
The target, and the rule that fights it
What a viable permanent magnet needs
1
μ₀Ms > 2 T
dense Fe/Co sublattice, little dilution
2
Tᴄ > 550 K
strong TM-TM exchange
3
Uniaxial anisotropy
needs the RE 4f crystal field
4
RE-lean, no critical elements
cost and supply
The Campbell rule
In metallic RE-TM intermetallics the 4f spin couples to Fe through a fixed chain:
4f spin ↔ own 5d (parallel, on-site)
5d ↔ Fe 3d (ANTIparallel, between sites)
Heavy RE (Gd–Tm): J = L + S, so the total moment follows the spin → antiparallel to Fe → ferrimagnet
Light RE (Nd, Sm, Pr): J = L − S, so the total moment opposes the spin → parallel to Fe → ferromagnet
Consequence: a genuinely ferromagnetic Fe-HREE phase is the exception, not the target to assume. The screen must test it, not presume it.
Outcome of the campaign: tested on 180 credible Fe/Co-Gd compounds - 180 ferrimagnets, 0 ferromagnets. The rule held everywhere; what varied, by 10x, was its strength.
Notes: Campbell rule: 4f-5d-3d chain fixes the sign. Heavy RE gives ferrimagnetism; light RE gives net-parallel alignment. This is why every database 'FM' label on a Gd-Fe compound deserves suspicion.

## Slide 3
SCREEN DEFINITION
Search criteria
1
Fe or Co ≥ 60 at.%
a dense 3d sublattice is the only route to >2 T; dilute phases cannot reach it
2
Contains one heavy RE
Gd, Tb, Dy, Ho, Er, Tm — the 4f source of anisotropy
3
Ternary compositions
keeps the phase space synthesisable and the DFT tractable
4
E above hull ≤ 0.2 eV/atom
on, below, or metastably above — many real magnets are metastable
5
Magnetic, or unknown
moment > 0.3 μᴮ/atom; 'no data' is kept, not discarded
6
Ordering decided by us
no database can answer FM vs ferri — that is the calculation
Criteria 5 and 6 are deliberately permissive: an unlabelled compound is a candidate, not a rejection.

## Slide 4
WHERE WE LOOKED
What each database can and cannot answer
Database | Hits | Filters natively | Key limitation
GNoME | 749 | composition, stability | no magnetic data at all; on-hull set only
Materials Project | 178 | ordering label, hull, moment | FM-initialised label; 4f frozen in core
OQMD | 283 | hull, composition | moments not exposed; structures via slow API
Alexandria | 73 | elements, nelements | moments response-only; server outages
AFLOW | 29 | spin per atom, species | no hull distance; thin RE-TM ternary coverage
The limitation they share
Every large database runs ONE spin-polarised calculation per structure, initialised ferromagnetically, with heavy-RE 4f frozen in the PAW core. So a “FM” label means “the Fe sublattice kept its moments” — never that the RE couples parallel. Nine FM-labelled Fe/Co-HREE candidates were found across all five databases; all nine contained Gd, the one heavy RE these codes treat explicitly.
Notes: The nine FM-labelled hits being all-Gd is a tell: it is an artefact of which element is treated with explicit 4f, not a physical discovery.

## Slide 5
THE SCARCE COMMODITY
Datasets that actually contain anisotropy
Source | What it uniquely has | Role in this campaign
Novamag | DFT K₁/MAE, exchange, Tc for RE-lean magnets | train + validate the MAE surrogate; calibrate A₂⁰
MAGNDATA | ~2,000 EXPERIMENTAL magnetic structures | ground truth for the fm/ferri coupling sign
C2DB | systematic MAE + exchange (2D materials) | benchmark an MAE model before trusting it in 3D
Heusler set (Sanvito) | ~236k compositions, moments + est. Tc | Tc training data; funnel-reporting template
Nelson–Sanvito Tc | ~2,500 experimental Curie temperatures | screen Tc before computing exchange constants
NIMS MatNavi / MDR | curated Nd-Fe-B and 1-12 experiment | validation targets (registration required)
Why these are worth more per entry
The five large databases we screened carry composition, stability and a moment. None carries MAE, exchange constants or Tc at scale — the quantities a permanent magnet is actually judged on. Novamag is the only open source of systematic anisotropy, which is what makes an MAE surrogate trainable at all.
Not open — do not plan around
MPDS / Pauling File and Springer Materials hold the deepest experimental magnet record, but neither is openly accessible.
Notes: Novamag: CC-BY-4.0, auto-fetched from Zenodo record 3241267 (160 MB). MAGNDATA is the strongest available test of the coupling-sign protocol - every experimental RE-TM entry is a check.

## Slide 6
FROM DATABASES TO CALCULATIONS
Screening funnel
554,055
GNoME stable entries scanned
1,152
unique candidate formulas across 5 databases
756
with retrievable crystal structures
352
compounds staged for DFT (24 native Gd + 328 Gd surrogates)
706
paired fm / ferri VASP calculations
726 parent compounds
collapse into 328
surrogate calculations
Deduplicated on (substituted formula, space group); coupling transfers back to each parent by de Gennes scaling.

## Slide 7
THE DECIDING CALCULATION
Two configurations, one energy difference
1
Pair every structure
Two collinear spin-polarised PBE+U runs, identical except the SIGN of the initial Gd moment: fm (+7 μᴮ) and ferri (−7 μᴮ).
→
2
Read the sign of ΔE
ΔE = E(ferri) − E(fm). Negative → ferrimagnetic ground state. Positive → genuine FM RE-TM coupling.
→
3
Transfer across the series
Tb–Tm ship as f-in-core potentials whose 4f cannot flip, so Gd is substituted onto every RE site and the result is carried back by de Gennes scaling, (gᴊ − 1)J.
Settings and controls
PBE+U Gd 4f U = 6.7 / J = 0.7 eV (U_eff = 6) · no U on metallic Fe · LASPH, LMAXMIX = 6 · ENCUT 520 · 8000 k-points·atom
Guards statics on a common geometry so ΔE isolates exchange · every run checked for SCF drift into the other spin state · light RE pinned to f-in-core so only Gd carries a flippable 4f · GdFe₂ (a known ferrimagnet) run as a protocol control

## Slide 8
PILOT — 16 RUNS, 8 COMPOUNDS
The protocol validates, and the database labels fall
Compound | Prototype | ΔE per Gd (meV) | Ground state | Net moment, ferri (μᴮ)
GdFe₂ (control) | Laves C15 | −352 | ferrimagnetic | −6.98
GdAlFe₄ | CaCu₅ RT₄X | −277 | ferrimagnetic | −0.03
GdGaFe₄ | CaCu₅ RT₄X | −284 | ferrimagnetic | 0.24
GdCo₄Si | CaCu₅ RT₄X | −155 | ferrimagnetic | −3.14
GdFe₄B | CaCu₅ RT₄X | −521 | ferrimagnetic | 1.08
GdCo₄B | CaCu₅ RT₄X | −263 | ferrimagnetic | −6.78
Gd₂Fe₃Co | Laves C14 | −329 | ferrimagnetic | −7.53
Gd₂Fe₁₂Ga₅C₂ | new, C2/m | −107 | ferrimagnetic | 8.53
Control passed
GdFe₂ is experimentally a ferrimagnet and the protocol reproduces that by 352 meV/Gd — which is what licenses trusting the rest.
Database FM labels were artefacts
GdAlFe₄ and GdGaFe₄ (Alexandria) and GdCo₄Si (MP) were all FM-labelled. All three are ferrimagnetic by 155–284 meV/Gd — and the two RT₄X phases are almost fully compensated, so their true net moment is ≈ 0, not the ≈1.9 T the FM-initialised numbers implied.
Notes: 8 of 8 pairs ferrimagnetic. 280 meV is far too large to be a convergence artefact. The compensation in RT4X is the practical kill: Fe sublattice ~14 muB cancels against Gd 7 muB x2 sites.

## Slide 9
SCALING THE SCREEN
Why the fm/ferri energies had to be forced apart before they could be trusted
The problem: a plain SCF doesn't stay where you put it
Each compound needs two static calculations - one initialised ferromagnetic, one ferrimagnetic - and the energy difference between them is the answer. At 353-compound scale, a plain unconstrained SCF too often drifts out of the state it was initialised in: LDA+U has several self-consistent solutions, and a simple collinear starting guess is not a strong enough anchor to hold either configuration in place through convergence.
The fix: lock the total moment, then release it
NUPDOWN fixes the total spin-up minus spin-down electron count, forcing the SCF to converge inside the intended basin. The target is derived from each element's own measured moment (not textbook values), never from a run already suspected of drifting.
1
Stage A - locked
NUPDOWN set to the intended fm/ferri moment; hardened mixing (NELM, EDIFF, AMIX); CHGCAR-only restart (WAVECAR skipped - it once cost 700 GB and failed ~60 runs on disk pressure alone)
2
Stage B - released
NUPDOWN removed; one final unconstrained static from Stage A's charge density - the energy actually compared, since a locked run only proves a state exists, not that VASP would choose it freely
The funnel this actually produced
353
compounds analysed
static fm/ferri pair, Gd surrogate
95
apparent ferromagnets
naive, unconstrained SCF result - taken at face value, most are not real
4
survive NUPDOWN hardening
measured-moment-derived locked rerun, released to a final unconstrained static
0
survive the release test
3 of the 4 carried multi-eV exchange energies (LDA+U multi-minima artefact); the 4th, Co16Gd2Mn, was a metastable Mn-parallel-to-Gd basin that released to a ferrimagnet
Notes: The 95->4 collapse on first hardening attempt actually went to ZERO credible - that first pass derived NUPDOWN from the same runs it was trying to fix (circular). Fixed by requiring a freely-converged reference or falling back to measured nominal per-element moments, split by high-spin/low-spin branch.

## Slide 10
CAMPAIGN RESULTS
No ferromagnet survives the release test; the false positive taught us the most
The funnel, after every validity rule
353
fm / ferri pairs staged
Gd stand-in for Tb-Tm, PBE+U, NUPDOWN-locked then released
180
credible exchange labels
both configs converged, TM and spectator sublattices stable, RE sites equal, exchange energy on a physical scale
180
ferrimagnetic
every credible pair: Gd antiparallel to Fe/Co, 28-371 meV per Gd
0
ferromagnetic
the Campbell 4f-5d-3d chain holds in all 180 - no host, decoration or Mn trick broke it
Co16Gd2Mn: the false positive, and why it was false
1
Locked relaxation
fm lower by 114.5 meV/Gd
the ferri reference had Mn parallel to Gd - a metastable spectator basin, held in place by the NUPDOWN lock and -42 kbar of residual pressure
2
Released statics
ferri (Mn ∥ Co) lower by 208 meV/Gd
E(ferri) = -146.088 eV vs E(fm) = -145.671 eV: a textbook Néel ferrimagnet once Mn is allowed to sit where it wants
3
Two Mn, four spin states
same ferrimagnet, 208 meV/Gd
Gd↓ Mn↑↑Co lowest; Mn forced against Co costs 1.25 eV per cell; Mn–Mn exchange ferromagnetic (B − A = 180 meV). Mechanism 2 closed at every site (18f, 18h, 9d, 6c)
What was learnt
A constrained calculation proves a state exists, not that nature picks it. Three validity rules were added to the analysis - spectator-flip detection, per-config convergence, RE-site equality - and only energies that survive an unconstrained release are compared. Under those rules the 180 credible pairs are a clean, systematic measurement of RE-TM exchange, which is worth more than one unverified ferromagnet.
Notes: Be explicit that the earlier deck claimed Co16Gd2Mn as FM. The release-stage comparison overturned it. The three validity rules now in analyze.py are the methodological product of that episode.

## Slide 11
THE Mn ARGUMENT, AND WHY IT FAILS
Right syllogism, wrong premise - and the corrected version cancels the magnet it tries to make
The original logic
1
Gd is antiparallel to Co because its 5d sees parallel 3d neighbours (Campbell).
2
Mn couples antiparallel to Co, so a Mn on the dumbbell next to Gd gives the 5d an antiparallel neighbour.
3
The 5d–3d rule then flips Gd to the Co side: ferromagnet, 1.95 T projected.
What the calculations said
Premise 2 is false here: Mn aligns WITH Co at 6c, 18f, 18h and 9d; opposing Co costs ~0.6 eV per Mn (state C, +1.25 eV for two).
The +114.5 meV compared fm against the Mn-against-Co basin, held by the NUPDOWN lock and −42 kbar. Released: ferri lower by 208 meV/Gd, same as without Mn.
One or two Mn cannot change what sixteen Co set: h, the summed shell polarisation, moved by < 10 %; the gap by 0 at two Mn.
The compensation argument: more Mn does not help either
Suppose Mn did oppose Fe/Co (true in Fe-rich hosts, R₂Fe₁₇₋ₓMnₓ). The Gd 5d follows the NET 3d spin of its shell: adding opposed Mn shrinks h and the gap, and Gd stays antiparallel to the net. At the crossover h → 0, but the net TM moment → 0 with it; past it Gd flips to oppose the Mn-dominated net. Gd is never parallel to the majority 3d moment, and the only point with no coupling is the point with no magnetisation. A Mn series measures a compensation curve, not a magnet.
Notes: Energies: Co16Gd2Mn released ferri (Mn||Co) -146.088 vs fm -145.671 eV; Mn-site twins released: 18f ferri_mnanti -145.886 vs fm -145.449; Co15Gd2Mn2 locked A -147.829, B -147.649, D -147.213, C -146.577 vs locked fm -147.414. Fe17Gd2H3 is the counter-example where the gap falls WITHOUT cancelling spin (H pushes the shell apart) - Ms survives but anisotropy is lost.

## Slide 12
WHAT THE 180 LABELS SAY · 1 / 2
The gap is not a neighbour count: the per-neighbour coupling itself varies 10-fold
How to read it
Each point is one compound: the fm/ferri energy gap per Gd against the summed moment of the Fe/Co atoms touching that Gd. If the RE-TM coupling were a universal constant, the points would sit on one dotted line.
What it shows
They span J_eff = 0.05 to 1.4 meV/μB²: at a fixed neighbour moment of ~25 μB the gap ranges from 110 to 370 meV.
The strongest coupling sits at LOW neighbour moment (Fe/Y and Fe+Co hosts, upper left), the weakest at high neighbour moment (2-17 hydride, lower right).
So neither coordination number nor TM moment predicts the gap. Something about the host, not the count, sets it.
Conclusion: a fixed J_RT times a neighbour count - the usual mean-field shortcut - would be wrong by up to 10x across this chemistry.

## Slide 13
WHAT THE 180 LABELS SAY · 2 / 2
Distance and chemistry set the coupling: short RE-TM bonds and mixed Fe+Co hosts couple hardest
Left: coupling falls as the Gd-TM distance grows (r = −0.61). Below 3.0 Å with 12 TM neighbours the Fe/Y hosts reach J_eff ≈ 1; above 3.15 Å - hydride, metalloid-shell and open cages - it drops to 0.05-0.4.
Right: mixed Fe+Co hosts have median J_eff 0.75 against 0.51 for pure Fe - Brooks' 5d-3d hybridisation argument seen on 27 compounds. The d-band centre and DOS at E_F add nothing once distance and the 5d moment are known (next slide).
Notes: Full OLS on log|dE|: 5d moment +0.34/SD, neighbour-sum +0.19, dilution +0.10, distance -0.04, d-band centre ~0; R2 0.63.

## Slide 14
THE 5d METHOD
Calibrated on 180 Gd pairs, the gap is read off a single calculation
Liebs & Fähnle (1993), used forward
ΔE = 2 · I₄f₋₅d · S₄f · S₅d
h = −½ [ m₅d(ferri) + m₅d(fm) ]
h is the part of the RE 5d moment tied to the TM neighbours; the part induced by the ion's own 4f flips with it and cancels. h is exactly what a 4f-free host (Y, or f-in-core Nd/Sm) reports as its RE moment.
|ΔE| = 1574 · h meV r = 0.89 I₄f₋₅d ≈ 225 meV
Why it matters
Circles mark the compounds with a measured exchange constant; stars are the gap their experimental J_RT implies. GdFe₂: J_RT 2.97 (ours) vs 2.99 × 10⁻²² J (expt). Validation slide follows.
Beats the raw ground-state 5d moment as a predictor (r 0.80 → 0.89) because it removes the 4f-induced part.
Turns an fm/ferri pair with 4f in the valence into ONE f-in-core run: J_RT, the RE molecular field B_RT = ΔE/2μ and T* = ΔE_RE/2k_B all follow.
Applied to Tao et al. 2026 (diamonds): Sm hosts predicted at 190-220 meV per Sm, T* 1100-1260 K - the Sm anisotropy stays locked to Fe up to Tc, consistent with their ferrimagnetic ground states.
Notes: Two outliers are circled: Gd2Fe17H3 far below the line (artifact suspect, in the suspects batch), and one Fe host far above (CFe17Gd2 - fm side suspect). Both are being re-run locked->released.

## Slide 15
VALIDATION AGAINST PRIOR WORK
Where literature gives a number, the campaign reproduces it
Quantity / rule | Literature | This campaign | Status
GdFe₂ RE-TM exchange J_RT | 2.99 × 10⁻²² J (Liebs, Hummler, Fähnle 1992; expt. molecular field) | 2.97 × 10⁻²² J from the fm/ferri gap (352 meV/Gd) | reproduced
ΔE ∝ S₅d (Liebs & Fähnle 1993) | shown on 3 compounds, ab initio | holds on 180 compounds, r = 0.89; I₄f₋₅d ≈ 225 meV | confirmed at scale
Campbell 4f-5d-3d sign rule | heavy RE always antiparallel to Fe/Co | 180 / 180 credible pairs antiparallel; 0 exceptions | confirmed
Duc's early-TM rule | V/Ti in GdFe₁₂₋ₓVₓ doubles A_GdFe (x = 0 → 4) | early-TM hosts J_eff ×0.97 of the Fe baseline (CI 0.88-1.07); GdFe₁₀V₂ J_RT 1.52 vs 1.30 expt | not resolved - needs a concentration series
Brooks: Co strengthens 5d-3d coupling | Co-based > Fe-based molecular fields | Fe+Co hosts J_eff 0.75 vs Fe 0.51, Co 0.57 | confirmed
Tao et al. 2026: Mn/Cr as weak-coupling mediators | Sm(Fe,Mn,Cr) hosts; RE moments −0.24 … −0.33 μB (f-frozen) | same h on our line → Gd-equivalent gaps 380-520 meV; hosts are strongly coupled, not weakly | reinterpreted
Mn-mediated RE-TM ferromagnetism (our own claim) | Co16Gd2Mn, +114.5 meV/Gd (locked) | Mn ∥ Co ferrimagnet by 208 meV/Gd after release | rejected
Learnt: the campaign is a quantitative instrument, not a yes/no screen. It reproduces the one measured RE-TM exchange constant it can be checked against, generalises the two-sublattice theory from three compounds to 180, and corrects its own headline when the release test disagrees.
Notes: Liebs-Hummler-Fahnle PRB 46, 11201 (1992); Liebs-Fahnle JMMM 128, L8 (1993); Duc 1998 review; Brooks-Johansson 5d-3d hybridisation; Tao et al. arXiv 2608.25270.

## Slide 16
VALIDATION AGAINST PRIOR WORK · THE NUMBERS
Four exchange constants with experimental values: three within 25 %, the control exact
What is compared
J_RT in the Liebs-Fähnle two-sublattice convention, ΔE = 4 J_RT S_R S_T Z_RT, computed from our fm/ferri gap with the compound's own TM moment and neighbour count - no fitted parameter.
GdFe₂
2.97 vs 2.99 - the protocol control, reproduced to 1 %.
Gd₂Fe₁₄B
1.84 vs 1.46 from inelastic neutron scattering - 26 % high; LHF's own LMTO value is 1.46, so the gap is in our Z_RT bookkeeping for the two inequivalent Gd sites.
GdFe₁₀V₂
1.52 vs Duc's A_GdFe 1.30 at x = 2 - 17 % high, and inside the spread of Duc's own series (1.13-2.25).
Gd₂Fe₁₇N₂ ↔ Ho₂Fe₁₇
1.21 vs 1.2-1.4 (Ho₂Fe₁₇, INS). Open marker: a nitride compared to a binary, because no Gd₂Fe₁₇ pair survived the validity rules.
Learnt: the campaign's exchange energies are on the experimental scale, biased ≤ 25 % high where the RE sites are inequivalent. Good enough to rank hosts; not yet good enough to resolve Duc's 15-20 % early-TM effect, which needs a concentration series on one lattice.
Notes: Sources: Liebs-Hummler-Fahnle PRB 46 11201 (1992) Table III (Loewenhaupt INS); Liebs-Fahnle JMMM 128 L8 (1993); Duc et al. JMMM 177-181 1107 (1998) Table 1. Ho2Fe17 used as the 2-17 reference since J_RT in this convention is nearly RE-independent.

## Slide 17
DESIGN PRINCIPLES, AUDITED
Every rule used to build permanent magnets, checked against the same 180 labels
Principle | What it predicts | What the dataset shows | Verdict
Heavy RE couples antiparallel (Campbell) | no FM Fe/Co-heavy-RE compound | 180/180 ferrimagnetic | confirmed
Gap scales with RE 5d spin (Liebs-Fähnle) | ΔE ∝ S₅d, host-independent I₄f₋₅d | r = 0.89 on h; d-band centre adds nothing | confirmed
de Gennes scaling across the RE series | ΔE_RE = ΔE_Gd · (g−1)J / 3.5 | assumed to project Tb-Tm and Nd/Sm; explicit-4f Tb-Tm runs under way | in test
Fe-rich, dense lattices for Ms | Ms ceiling set by Fe density | best Gd hosts 0.9-1.06 T; light-RE projection ceiling ≈ 1.75 T (0 K, no SOC) | confirmed
Light RE (J = L − S) adds to Ms | Nd/Sm moment parallel to Fe | projected +0.6-0.9 T over Gd; 20 f-in-core runs queued | in test
Interstitial N / C raise Ms and Tc | lattice expansion, stronger Fe-Fe | Gd₂Fe₁₇N₂ is the top Ms host; C analogues close behind | confirmed
Interstitial H is harmless | mild expansion only | Gd₂Fe₁₇H₃ gap 28 meV (×0.10): H in the RE shell nearly switches off RE-TM coupling - one compound, re-running | rejected if it survives release
Early-TM stabilisers (Ti, V, Zr, Nb) help | stabilise 1:12-type cells, stronger coupling (Duc) | coupling ×0.97 of baseline, no effect resolved; hull: Fe₅GdV on hull, Ti variants 12-19 meV above | stability yes, coupling unresolved
Partial Co for Tc and coupling | Co raises Tc and RE-TM field | Fe+Co hosts strongest J_eff (0.75); Ms cost small at low Co | confirmed
Mn as a sign-flipping mediator | Mn ∥ RE breaks the antiparallel rule | Mn ∥ Co in every released state | rejected
Metalloid-rich cages (B, Si, Ga, Al in RE shell) | stabilise structures cheaply | systematically lower gaps - anisotropy decouples first | use with care
Learnt: most principles hold in direction but their magnitudes differ by an order of magnitude, one (early TM) is not resolved by cross-host data, and only the 5d-spin rule is quantitative enough to rank candidates.

## Slide 18
DESIGN PRINCIPLES, AUDITED · EFFECT SIZES
The same rules as numbers: how far each lever moves the RE-TM coupling from the Fe baseline
Reading the chart
Median J_eff of the compounds carrying a lever, divided by the median of all 123 Fe-only hosts; bars are bootstrap 95 % intervals. Blue = strengthens coupling, red = weakens, grey = not resolved.
×1.48 partial Co
the only lever with a large, resolved positive effect
×1.12 all-Co
modest; Co also lowers Ms, so partial Co is the useful form
×0.97 early TM
Duc's effect is not visible across different hosts; it needs a series on one lattice
×0.86 distance > 3.15 Å
open cages weaken coupling, consistent with the 5d picture
×0.10 H interstitial
one compound, under re-check; if real, the strongest lever of all - in the wrong direction
Learnt: of the levers the field uses, only partial Co and short RE-TM bonds measurably raise the RE-TM coupling in this dataset. Metalloids are neutral on average; their harm is specific to sitting in the RE shell. The early-TM rule is a stability lever until a concentration series says otherwise.

## Slide 19
HYPOTHESIS: THE LEVERS COMPOSE
Hypothesis: a strongly coupled Gd host plus a light rare earth is a hard-magnet candidate
180
credible Gd hosts
the labelled dataset
96
project ≥ 1.4 T with Nd
Fe sublattice moment + free-ion Nd, same cell
70
not a known prototype
drop Nd₂Fe₁₄B, 2-17(N,C,H), Laves, Th₂Zn₁₇, the Mn family
29
strongest coupling, Fe-rich
J_eff ≥ 0.5 or gap ≥ 300 meV; 1:9 family by 3 representatives
20
survive the hull, Nd + Sm
MACE-MP-0 vs 394 MP competitors, same model; Nd within 12 meV/atom
Generation rule: host with gap ≥ 250 meV or J_eff ≥ 0.5 × Gd → {Nd, Sm} × keep Co/early-TM variants × no H, no metalloid in the RE shell → MACE/MP hull → one f-in-core VASP run. 29 hosts → 58 structures → 20 survivors; the rule extends to Pr, partial Co and N interstitials once this batch confirms it.
First test of the hypothesis: the Nd cost is systematic (20-35 meV/atom for the larger ion), so only the densest Fe hosts stay on the hull; Sm is nearly free. Whether coupling and Ms carry over is what the 20 queued runs decide.

## Slide 20
THE Nd / Sm BATCH - 20 RUNS QUEUED
Each host carries a reason from the data, a stability check, and a prediction to be tested
Host (Gd parent) | Prototype | J_eff | Ms → Nd / Sm (T) | E_hull Nd / Sm (meV/at) | T* Sm (K) | Why it is in the batch
Fe₅GdSi | Immm (new) | 0.50 | 1.74 / 1.56 | +1 / −6 | 700 | highest Ms of any stable new host; Si outside the RE shell
Al₂Fe₁₀Gd | Immm (new) | 0.54 | 1.68 / 1.51 | +3 / −3 | 745 | same Fe framework, Al variant; tests the metalloid-shell rule
Fe₅GdV | Immm (new) | 0.48 | 1.62 / 1.44 | +7 / +2 | 715 | early-TM lever built in (Duc); 1:12-like chemistry
Fe₁₀GdY | Pmmm (new) | 0.52 | 1.64 / 1.47 | +11 / +3 | 825 | dense Fe, Y dilutes RE cost
CoFe₆GdY | Cm (new) | 0.97 | 1.59 / 1.37 | +10 / −5 | 955 | strongest coupling at Ms > 1.5 T; partial Co
Co₂Fe₁₂GdY₃ | Cm (new) | 1.04 | 1.44 / 1.33 | +1 / −8 | 1005 | anisotropy-locking host; on the hull
CoFe₁₃GdY₃ | R3m (new) | 1.03 | 1.42 / 1.31 | +7 / −3 | 1030 | Fe/Y family, 12-fold RE coordination at 2.97 Å
Fe₁₄GdY₃ | R3m (new) | 1.06 | 1.40 / 1.29 | +11 / −1 | 1070 | Co-free control for the two above
Fe₉GdLuZr | R3m (new) | 0.51 | 1.48 / 1.27 | +9 / −3 | 810 | 1:9 family representative with Zr stabiliser
Co₉Fe₅Gd₄ | R-3m (new) | 0.69 | 1.69 / 1.23 | +3 / −16 | 725 | RE-rich control: high Nd moment count, lowest Tc expected
What each run returns
One ISIF=3 relaxation per compound with f-in-core Nd_3 / Sm_3 (no 4f to flip, no +U): relaxed volume, Fe/Co moments → Ms, and h → predicted gap, T*, B_RT. Prediction on record before the run: h from each Gd parent's pair.
Honest ceiling
Projections are 0 K PBE without SOC and run ≈ 0.3 T high against experiment (Nd₂Fe₁₇Nₓ: 2.04 projected vs ~1.5 T). None of the 20 beats NdFe₁₂N (1.66 T, Tc 823 K) or Sm(Fe,Co)₁₂ (1.78 T). Their value is as new, hull-stable Fe-rich hosts with coupling strong enough to carry RE anisotropy - the ingredient the 2 T target has lacked.
Notes: Job 59642825, 20 nodes, 3 h, regular QOS, submitted 2026-10-10 11:58. Reader: light_re_results.py. Tc is NOT in this batch - it needs an Fe-Fe Heisenberg mapping, planned as the next step for survivors.

## Slide 21
NEW HYPOTHESES
What prior studies plus 180 labels let us state - each falsifiable with runs already queued or cheap to add
H1
The RE-TM gap of any host is predictable from a 4f-free calculation
h measured in the f-in-core Nd/Sm run equals h extracted from the Gd pair of the same host, and 1574·h reproduces the Gd gap within 20 %. Falsified if the 20 queued runs scatter off the line.
H2
Usable anisotropy needs T* above Tc, and T* is a host property
Hosts with gap < ~150 meV per Gd (H-loaded, metalloid-shell, open cages) lose RE anisotropy below Tc regardless of RE choice. Testable on the suspects batch and by SOC runs on two low-gap vs two high-gap hosts.
H3
Partial Co in Fe/Y hosts buys coupling at almost no Ms cost
Fe+Co hosts have 50 % higher J_eff; at ≤ 15 % Co the Fe moment barely drops. Prediction: CoFe₆NdY and Co₂Fe₁₂NdY₃ show higher h than Fe₁₄NdY₃ at similar Ms. Direct comparison inside the batch.
H4
The compound lever is light RE + early TM + N interstitial on a dense new host
Light RE, partial Co and N are each supported by the data; early TM is a stability lever whose coupling effect is unresolved. None has been combined on a hull-stable new prototype. Fe₅(Nd,Sm)(Si,V) Immm with N on the largest void is the first test - MACE hull, then one run.
H5
Interstitial choice is a coupling decision, not just a volume decision
N and C expand the lattice and keep the gap; H in the RE shell collapses it. Hypothesis: the interstitial's site relative to the RE, not its size, decides. Test: H vs N on the same 2-17 cell, same site.
Each hypothesis names its own disproof. H1 and H3 are decided by the batch now in the queue.

## Slide 22
EXTENDING THE GD DATASET
Using Campbell's rule to predict the rest of the series
What the Gd calculation gives you
ΔE from the fm/ferri pair is the RE-TM exchange energy itself. Because the sign is fixed by the 4f-5d-3d chain and only the 4f spin magnitude changes down the series, one Gd pair predicts all six heavy rare earths.
coupling strength
J(RE–TM) ∝ (g_J − 1) J
Tc contribution — de Gennes factor
G = (g_J − 1)² J(J + 1)
Gd 15.75 · Tb 10.5 · Dy 7.08 · Ho 4.5 · Er 2.55 · Tm 1.17
net moment
M_net = M_TM − n_RE × g_J·J
The Fe sublattice moment carries over unchanged; only the RE terms rescale — so both Tc and net moment are predictable for Tb–Tm without new calculations.
1
Rank by uncompensated moment, not by FM
For every Gd result, evaluate M_TM − n_RE·g_J·J across the series. High Fe:RE ratios (2-17, 1-12) leave a large residual; RT₄X compensates to ≈ 0. This reprioritises the whole candidate list at zero DFT cost.
2
Hunt where the 5d-3d chain breaks
The antiparallel sign is mediated by RE 5d. Screen for phases where that channel weakens: semiconducting or semimetallic X, long RE-Fe distances, RE coordinated only by anions, dilute RE. These are the only plausible FM exceptions.
3
Use the induced 5d moment as a free diagnostic
Every Gd run already reports the RE 5d moment. Where its sign or magnitude deviates from the usual antiparallel pattern, the mechanism is weakening — a cheap flag for which compounds deserve explicit Tb–Tm treatment.
4
Escalate only the outliers
Explicit 4f Tb–Tm with occupation-matrix control is expensive and fragile. Reserve it for de Gennes outliers and predicted FM exceptions, then add Tᴄ via exchange constants for survivors.
Notes: Key reframing: the Gd campaign is not just a yes/no on ferromagnetism. It is a measurement of the RE-TM exchange that propagates to the whole heavy series analytically.

## Slide 23
CAMPBELL'S RULE, APPLIED
Which results reach the target with which rare earth, against magnets on the market
How to read it
One row per host, ranked by its Nd projection. The Fe/Co sublattice moment is the computed one; each marker swaps the RE: Gd as computed (ferri), heavy Tb/Dy antiparallel, light Nd/Sm parallel. Dotted lines: measured Ms of commercial and benchmark magnets.
Heavy RE never works
Tb/Dy pull every host below 1 T; most go negative (RE-dominated).
Light RE recovers 1.4-2.0 T
the known 2-14-1 and 2-17-N hosts top out at 2.0 T projected ≈ 1.6-1.7 T real; Nd₂Fe₁₄B and NdFe₁₂N are exactly that.
New hosts land at 1.7-1.9 T
CoFe₁₃NdY₃, Co₇Fe₁₆Nd₆, Fe₅NdSi, Fe₁₁NdW - the first two are RE-rich, the last two are the queued batch.
Sm costs 0.2-0.4 T
but carries the strongest anisotropy and sits on the hull more often.
Learnt: within this chemistry the rare earth sets Ms far more than the host does; the host's job is coupling strength and stability, which is why the batch was chosen on those two and not on Ms alone.
Notes: All projections are 0 K PBE without SOC and ~0.3 T above experiment (Nd2Fe17Nx 2.04 projected vs ~1.5 measured). Literature: Nd2Fe14B 1.61 T/585 K; Sm2Fe17N3 1.54/749; NdFe12N 1.66/823 (Hirayama 2015); Sm(Fe0.8Co0.2)12 1.78/859 (Hirayama 2017); Sm2Co17 1.25/1190.

## Slide 24
AFTER THE COUPLING QUESTION
How much Gd must be replaced to make a magnet
The gap the campaign leaves
Gd is a 4f⁷ S-state ion: L = 0, spherical charge cloud, no single-ion anisotropy by construction. That is exactly why it is a clean surrogate for exchange — and exactly why it can never be the final composition.
κ = √( K₁ / μ₀Ms² ) ≥ 1
μ₀Ms | K₁ for κ = 1 | K₁ for κ = 1.54
1.5 T | 1.8 MJ/m³ | 4.2 MJ/m³
2.0 T | 3.2 MJ/m³ | 7.5 MJ/m³
Higher Ms demands MORE anisotropy, not less — which is why a 2 T target forces a non-spherical 4f ion. (κ = 1.54 is Nd₂Fe₁₄B.)
1
Inputs
|ΔE| per Gd from the campaign sets the exchange field; Stevens α_J and ⟨r²⟩ are tabulated. Only A₂⁰, the crystal-field parameter at the RE site, must be computed separately.
2
Model
K₁(x,T) from the 2nd-order crystal field with the Callen–Callen l = 2 law (K₁ ∝ m_RE³); Ms(x) from the TM sublattice and the RE moments, signed by the coupling.
3
Solve
smallest x clearing κ ≥ 1 at operating temperature. Example: A₂⁰ = +300 K/a₀², 450 K → Tb at x = 0.77 gives K₁ = 5.7 MJ/m³, μ₀Ms = 2.67 T, κ = 1.0.
4
Keep Gd for Tc
Gd has the largest de Gennes factor of the series (15.75 vs Tb 10.5, Dy 7.08), so it contributes most to Tc. Target the MINIMUM x that clears the bar.
Two traps the solver enforces: only ONE Stevens sign family is easy-axis for a given A₂⁰ (Tb/Dy/Ho have α_J < 0, Er/Tm α_J > 0 — mixing them cancels), and K₁ < 0 is easy-plane, which is not a magnet at any magnitude.
Notes: A20 sign convention must be calibrated against a known compound first. Novamag is the natural calibration source.

## Slide 25
THE PHYSICS BEHIND THE DESCRIPTORS
Each descriptor and threshold in the workflow stands for a known principle; here is which, and what we measured
Principle (source) | What it says | Descriptor / rule in the workflow | Our evidence
Campbell 4f–5d–3d chain (Campbell 1972) | RE 4f polarises its own 5d; 5d–3d coupling is antiparallel → heavy RE ferri, light RE parallel | RE one-hot; light RE (Nd, Sm, Pr) only in the waves; sign never fitted | 180/180 Gd pairs ferrimagnetic
Two-sublattice exchange, ΔE = 2 I₄f₋₅d S₄f S₅d (Liebs, Hummler, Fähnle 1992; Liebs & Fähnle 1993) | the RE–TM gap is set by the 5d spin the host induces on the RE | label h = TM-tied 5d polarisation; gap = 1574·h (the GP target) | r = 0.89 on 180 compounds; GdFe₂ J_RT 2.97 vs 2.99 × 10⁻²² J
5d–3d hybridisation (Brooks & Johansson) | shorter RE–TM bonds and more 3d states at the RE raise the 5d polarisation; Co > Fe | d_RE-TM mean/min, N_TM_nn, f_Co, 3d count | distance r = −0.61; Fe+Co J_eff ×1.48
de Gennes scaling (de Gennes 1962) | RE–TM coupling ∝ (gJ−1)J; Tc contribution ∝ (gJ−1)²J(J+1) | gap_RE = gap_Gd·(gJ−1)J/3.5 → T* threshold per RE | Tb–Tm projected from Gd; explicit-4f check running
Early-TM enhancement (Duc 1998) | Ti, V on the TM site raise the RE–TM exchange and stabilise 1:12 | f_early; early-TM substitution on the far Fe site | stability yes; coupling ×0.97, needs a series
Slater–Pauling / magnetic valence (Williams, Malozemoff, Moruzzi 1983) | Ms is set by Fe density and the 3d count; Co, early TM and p-elements lower the moment | tm_density, f_Fe, d_count, x_dil → analytic Ms; Ms ≥ 1.5 T filter | Ms ceiling 1.75 T projected; kagome capped at 1.0 T
Interstitial modification (Coey & Sun 1990) | N, C in the RE-adjacent void expand the lattice, raise Ms and Tc, keep the RE coupling; H does not | n_N/C/H in the RE shell; interstitial generator on the 2b / 9e voids | H: gap ×0.10; C passes the hull, N does not
Metastability scale (Sun, Ceder et al. 2016) | synthesisable phases sit within tens of meV/atom of the hull; MLIP error ≈ 30 meV | same-model MACE/MP hull; E_hull ≤ 30 meV filter | Nd costs 20–35 meV vs Gd; Sm ≈ free
RE anisotropy needs a locked RE sublattice (Kuz'min; Coey) | the 4f crystal-field anisotropy only works below the RE–TM decoupling temperature | T* = gap_RE/2k_B ≥ Tc target → gap_RE ≥ 100 meV (Nd₂Fe₁₄B level) | Tao hosts: T* 1100–1260 K for Sm
None of these is new; what is new is that one dataset tests all of them at once and turns them into numbers a surrogate can use.
Notes: Refs: Campbell J. Phys. F 2, L47 (1972); Liebs, Hummler, Fahnle PRB 46, 11201 (1992); Liebs & Fahnle JMMM 128, L8 (1993); Brooks & Johansson, Handbook of Magnetic Materials 7 (1993); de Gennes J. Phys. Radium 23, 510 (1962); Duc et al. JMMM 177-181, 1107 (1998); Williams, Malozemoff, Moruzzi JAP 54, 3129 (1983); Coey & Sun JMMM 87, L251 (1990); Sun et al. Sci. Adv. 2, e1600225 (2016); Kuz'min & Tishin, Handbook of Magnetic Materials 17 (2008). Benchmarks: Hirayama et al. Scripta Mater. 95, 70 (2015) NdFe12N; Hirayama et al. Scripta Mater. 138, 62 (2017) Sm(Fe,Co)12; Korner, Krugel, Elsasser Sci. Rep. 6, 24686 (2016) HT 1:12 screening.

## Slide 26
THE PRINCIPLES AT WORK
Five compounds from the pool, and which principle decided their fate
Brooks–Johansson in the data: coupling vs RE–TM distance and vs host class, 180 labels
Fe₅NdSi · Immm
in wave 1
short RE–TM bonds (2.97 Å, 12 TM) → GP predicts h 0.15, gap 82 meV; Fe density → 1.74 T; on the hull
Brooks–Johansson · Slater–Pauling · hull
Gd₂Fe₁₇H₃
excluded by design
H in the RE first shell → measured gap 28 meV; descriptor n_H_shell flags it; no H variants are generated
Coey interstitial rule, inverted
Co₁₉Fe₄Gd₆
Co variants generated for every host
mixed Fe+Co host → strongest coupling in the set, J_eff 1.41; on the Pareto front
Brooks: Co strengthens 5d–3d
Nd(FeGe)₆ kagome
fails Ms floor; none drawn
stable (−7 meV) but TM density 3.2 per 100 Å³ → Ms 1.0 T; RE in a 3.3 Å channel → weak coupling
Slater–Pauling density · Brooks distance
(Pr,Nd)Fe₁₀.₅V₁.₅N
V cells in wave 1; nitride needs an exception
1:12 with V stabiliser, mixed RE, N in the 2b void - the real magnet composition; N variant above the hull cut
Duc · de Gennes · Coey · Sun metastability
What the principles cannot do, and the loop does
Each rule gives a direction, not a magnitude, and they conflict: Co raises coupling but lowers Ms; early TM stabilises 1:12 but dilutes Fe; N raises Ms but leaves the hull. The GP learns the magnitudes from the 180 labels, Thompson sampling resolves the conflicts under the thresholds, and every wave returns the measurements that correct the rules themselves.
Notes: Fe5NdSi numbers from wave_1.csv; Gd2Fe17H3 from results.json (suspects batch re-running it); Co19Fe4Gd6 from exchange_features.csv; kagome from pool.csv; mixed 1:12 from generate_mixed_1_12.py / pool.csv.

## Slide 27
THE WHOLE LOOP ON ONE PAGE
Standard flowchart: data in cylinders and parallelograms, decisions in diamonds, the HPC step in red
START
prototypes +
databases
structure store
GNoME · MP · OQMD
+ generated cells
substitute
Nd/Sm · Co · early TM
N/C interstitials
MACE-MP-0
relax cell
(30 s)
E_hull ≤ 30 meV
and Ms ≥ 1.5 T ?
archive
(training only)
no
yes
pool row
15 geometry descriptors
+ RE one-hot
GP predicts h
(5d polarisation):
linear trend + GP correction
Thompson sampling
→ wave of 120
(constraints + cap)
VASP on Perlmutter
120 f-in-core relaxations
one packed 4 h job
per run: h, Fe/Co moments, V
→ gap_RE = 1574·h·(gJ−1)J/3.5
T* = gap_RE/2k_B, Ms = Σm/V
ingest: parse OUTCARs →
labels.csv; compare measured h
to predicted (H1); re-fit GP
Pareto front
moved? feasible
candidates left?
END → candidate list
SOC anisotropy → Tc
→ synthesis
no
yes
retrain on new labels
expand: winners × levers
→ new cells into the store
behind the GP label: gap = 1574·h on 180 Gd pairs, r = 0.89 - one f-in-core run per label
behind the hull decision: MACE vs MP competitors, Ms vs stability for the light-RE hosts
Notes: Standard symbols: terminator = start/end, rectangle = process, diamond = decision, parallelogram = data, cylinder = stored data. Red process = the only HPC step. Solid loop = retraining; dashed loop = neighbourhood expansion of the winners feeding the structure store.

## Slide 28
GENERATING CANDIDATES
Polytypes we decorate, and the substitutions we apply to them
Polytypes (prototype → generated cells)
CaCu₅ · RT₄X (SmCo₅ family)
X site decorated; compensates near 0 T, kept for coupling
61
ThMn₁₂ · RFe₁₁X, RFe₁₀X₂ (1:12)
stabiliser X = Ti V Cr Zr Nb Mo W Hf Ta Re
21
Th₂Zn₁₇ / Th₂Ni₁₇ (2:17) + interstitials
the Sm₂Fe₁₇N₃ framework
21
Nd₂Fe₁₄B / Nd₂Fe₁₄C (2:14:1)
the reference magnet lattice
20
LaCo₉Si₄ (1:9)
dense 1:9 R3m family
21
Kagome RT₆X₆ · HfFe₆Ge₆-type
Fe₆, Co₆, Fe₅Co × Sn Ge Si Ga Al; + vacancy
30
Nitrides / carbides of the passers
N, C in the RE-adjacent void: 2b, 9e, GNoME channels
224
Mixed-RE fractional 1:12 (Nd,Pr,Sm)₂Fe₂₁V₃N₀₋₂
the real NdFe₁₂-based composition class
9
GNoME frameworks (new-R3m, R-3m, Cm, Immm …)
campaign hosts, light-RE substituted
369
gold = added this week from the data-backed levers
Substitutions (site → palette → why)
Site | Palette | Reason from the data
RE site | Gd → Nd, Sm; Pr in expansion; Nd/Pr/Sm pairs | light RE adds to Ms (J = L − S); Sm couples harder (×1.46 gap)
TM site, nearest the RE | Fe → Co at ⅛ and ¼ | partial Co: coupling ×1.48, the only large resolved lever
TM site, farthest from RE | Ti V Cr Zr Nb Mo W Hf Ta Re (one atom) | 1:12 stabiliser pattern; coupling effect unresolved (×0.97)
Prototype X site | Al Si Ga Ge B C N P Sn Sb Zn Cu | the classic decoration palette; metalloids neutral on average
RE-adjacent void | N, C - dilute and fully occupied | Ms and Tc lever of Sm₂Fe₁₇N₃ / NdFe₁₂N; keeps the gap (unlike H)
Channel X (kagome) | one X removed | the defective 1:6:6 variant seen experimentally
Not applied | H interstitial · Mn · Dy · U | H kills coupling (×0.10); Mn ∥ Co, no gain; Dy via de Gennes only; U out of scope
Every variant → MACE relax → same-model hull → descriptors → pool. Generation is cheap (30 s per cell); the thresholds and the GP do the selecting.
Notes: Counts: 146 original decorations (first six rows of the old slide 24, by prototype), 30 kagome, 224 interstitial cells on 60 Fe-rich passers, 9 mixed 1:12 supercells, 369 campaign host structures (180 credible + 189 unlabelled).

## Slide 29
TWO LOOPS
An operational loop that proposes and tests; an understanding loop that explains and feeds back
Generators
prototypes · levers · neighbourhood of winners
(pool = 1,427 cells)
MLIP filter
MACE relax · same-model hull
E_hull ≤ 30 meV · Ms ≥ 1.5 T
GP surrogate
mean = physics rules
+ Matern residual on h
Acquisition
batch Thompson sampling
+ contrast slots that resolve
open causal questions
DFT, then experiment
one f-in-core run per cell
→ h, Ms, V (ground truth)
Understanding loop: interpretable pipeline on every label
effect sizes (what each lever does) → causal graph (host → S₅d → gap; Fe density → Ms) → symbolic rule (ΔE = 1574·h, de Gennes scaling) → checked against literature constants
DFT results
sets the mean function
disambiguation targets
which levers to generate
labels retrain the surrogate every round
Loop 2 so far: 'the gap is set by h' became the GP mean and the one-run label · 'H kills coupling, Co raises it, early TM unresolved' became the generator levers and a contrast target (an early-TM series on one lattice) · 'Mn cannot flip the sign' retired a whole branch.
Notes: Adapted from the two-loop picture (operational loop + causal/interpretable loop). Differences in NEEL: the MLIP filter sits BEFORE the GP (constraints first, surrogate on survivors); generation precedes acquisition (one cannot score what does not exist), with the generator conditioned by loop 2's levers; the interpretable pipeline is effect sizes -> hand-specified structural causal model validated on the data -> symbolic rule, rather than a long tool chain (RF/SOM/EBM/SymReg/LogReg/ENCO), because 180-300 labels in 15-19 dimensions do not support data-driven causal discovery; 'disambiguation targets' are implemented as contrast experiments (same host, one lever changed) that the acquisition reserves slots for.

## Slide 30
TWO LOOPS, EXTENDED
Same loops, two additions: a conditional diffusion generator, and a fuller interpretable pipeline feeding it
Generators
rule-based (now)
+ conditional diffusion model
(MatterGen / DOSMatGen class)
NEW
MLIP filter
MACE relax · same-model hull
E_hull ≤ 30 meV · Ms ≥ 1.5 T
GP surrogate
mean = extracted rules
+ Matern residual on h
Acquisition
Thompson batches
+ disambiguation slots
+ 'novelty' slots for generated cells
DFT, then experiment
one f-in-core run per cell
→ h, Ms, V (ground truth)
Understanding loop: interpretable pipeline RF → SOM → EBM → SymReg → LogReg → ENCO
RF
random forest on the labels: which descriptors carry the signal (done: 5d polarisation, distance, Co)
SOM
self-organising map: cluster hosts into families; shows which families the waves have not sampled
EBM
explainable boosting: additive per-descriptor curves - the shape of each lever, not only its sign
SymReg
symbolic regression: closed forms (done by hand: ΔE = 1574·h; next: h = f(distance, Z, Co))
LogReg
feasibility classifier: P(hull ∧ Ms ∧ gap) from geometry - a cheap pre-filter before MACE
ENCO
causal discovery using the waves as interventions: tests the hand-built graph (host → S₅d → gap) and finds edges we missed
DFT results
rules → mean
disambiguation targets
causal parents = conditioning variables
GP posterior → inverse design toward the empty Pareto corner
Minor modifications, in order: (1) add the diffusion model as one more generator - its proposals enter the same MLIP filter and the same GP; (2) condition it on the variables the causal graph names as parents of coupling and Ms, so it proposes short-bonded, Fe-dense, Co-tuned, H-free frameworks; (3) reserve acquisition slots for generated cells so novelty is sampled, not just exploited; (4) once waves give interventional data, run ENCO to audit the hand-built graph. Nothing downstream of the generator changes.
Notes: Pipeline names follow the two-loop slide shared by the user: RF = random forest, SOM = self-organising map, EBM = explainable boosting machine, SymReg = symbolic regression, LogReg = logistic regression, ENCO = Efficient Neural Causal Discovery (Lippe et al. 2022), which uses interventional data - here each wave's substitutions are the interventions. Caveat: with a few hundred labels the data-driven causal discovery should be read as an audit of the hand-specified SCM, not a replacement for it.

## Slide 31
CANDIDATE GENERATION
Seven sources feed one pool; every structure gets the same relaxation, hull and descriptors
Database structures
GNoME · MP · Alexandria · OQMD
903 formulas with a CIF
+147 recovered this week (MP by id)
134 in pool
Campaign hosts
180 credible Gd hosts (all, not only strong)
+189 compounds without a credible label
(f-in-core has no +U: they converge)
656 in pool
Prototype decoration
CaCu₅-RT₄X, ThMn₁₂, Th₂Zn₁₇, Nd₂Fe₁₄B,
LaCo₉Si₄ × 19-element X palette
146 Gd cells → Nd and Sm
252 in pool
Kagome RT₆X₆
HfFe₆Ge₆-type P6/mmm; Fe₆, Co₆, Fe₅Co
× Sn, Ge, Si, Ga, Al; + channel vacancy
(none passes Ms ≥ 1.5 T: Fe density 3.2)
60 in pool
Interstitial N / C
largest RE-adjacent void of every Fe-rich
passer (2b in 1:12, 9e in 2:17, GNoME
channels); dilute + full occupation
224 cells
Mixed-RE fractional 1:12
2-f.u. supercells: (Nd,Pr,Sm)₂Fe₂₁V₃N₀₋₂
= RFe₁₀.₅V₁.₅N₀₋₁, the real magnet
composition class
9 cells
Neighbourhood expansion
after each wave: top-25 labelled winners
× RE swap, Co ⅛ and ¼, early TM on the
far Fe site, N - the data-backed levers
wave ≥ 2
The pool today
1,427 unique structures relaxed
all with a same-model hull energy
~140 pass hull ≤ 30 meV and Ms ≥ 1.5 T
→ Thompson sampling drew wave 1 (120)
Generated ≠ stable: database candidates arrive with a hull distance, generated ones do not - which is why every source goes through the MACE hull before the GP ever sees it (next slide).
Learnt from building the pool: the generators that add feasible candidates are the Fe-dense ones (2:17, 1:12, 3:29 frameworks, their nitrides and Co variants); kagome and metalloid-rich cages are stable but cannot reach 1.5 T. Generation is cheap, so breadth costs nothing - the thresholds do the selecting.
Notes: Counts from analysis/pool/pool.csv at the time of the wave-1 redraw. Dedupe is on (reduced formula, space group); the same host can appear from several sources, the lowest-hull copy is kept.

## Slide 32
FROM PROTOTYPE TO POOL ROW
Substitution rules, then two surrogate screens, then descriptors - no DFT until the wave
Source cell
heavy-RE placeholder (Gd)
or light-RE cell from a
generator
Substitution rules
Gd → Nd, Sm (Pr in expansion)
Fe → Co, ⅛ nearest the RE
early TM on the far Fe site
N / C into RE-adjacent voids
Dedupe
(reduced formula,
space group)
lowest hull kept
MACE-MP-0 relax
cell + positions
fmax 0.1 eV/Å, ≤120 steps
~30 s per cell on CPU
Same-model hull
MP competitors ≤100 meV
re-relaxed with MACE
→ E_hull
Descriptors
15 geometry numbers
+ RE one-hot
(wave_features.py)
Analytic Ms
Σ TM moments (campaign
medians) + free-ion RE
÷ relaxed volume
pool.csv row
cid · formula · source
E_hull · Ms · descriptors
→ POSCAR_mace
Hard filters
E_hull ≤ 30 meV/atom
(MACE noise ≈ 30)
Ms_proj ≥ 1.5 T
→ GP + sampling
feasible set
(94 of 1,220 today)
next slide
The 15 descriptors (all pre-DFT): N_TM_nn, d_RE-TM (mean, min) · f_Fe, f_Co, 3d count, TM per RE, dilution · TM density, volume per atom · early-TM fraction · metalloid / H / N / C atoms in the RE shell
Why two surrogates: MACE answers 'does this cell exist' (stability, geometry) at 30 s per structure; the GP answers 'is it worth a VASP run' (coupling) from the geometry MACE produced. Neither replaces the DFT label - they decide which 120 of the 1,220 get one.

## Slide 33
THE GP, WHAT IT FITS, HOW IT PICKS
Two-stage model on the 5d polarisation h; batch Thompson sampling under the magnet constraints
1 · Training rows
179 credible Gd pairs: label h = −½[m₅d(ferri) + m₅d(fm)]
+ every ingested f-in-core wave run: h read directly
features = 15 descriptors + RE one-hot, standardised
2 · Mean function (ridge)
w = argmin ‖h − Xw‖² + α‖w‖², α = 1
the physics the 180 labels already fixed:
distance, coordination, Co fraction, dilution
3 · GP on the residual r = h − Xw
k = σ²·Matern₅⁄₂(ℓ₁…ℓ₁₉) + σₙ²
hyperparameters maximise the log marginal likelihood
log p(r|X) = −½ rᵀK⁻¹r − ½ log|K| − (n/2) log 2π
→ posterior mean μ(x), std σ(x)
4 · Stage two (deterministic)
gap_RE = 1574 · h · (gJ−1)J_RE / 3.5
T* = gap_RE / 2k_B
Ms from the pool row (analytic)
no fitted parameter beyond 1574
5 · Validation before use
10-fold CV on the 179 Gd labels:
r = 0.88, RMSE 0.018 μB (label sd 0.038)
91 % of held-out labels inside ±2σ
H1 check on every wave: measured h vs predicted
6 · Batch Thompson sampling
per pick: one joint posterior draw h̃ over the pool
feasible if gap̃_RE ≥ 100 meV, Ms ≥ 1.5 T, E_hull ≤ 30
utility U = Ms · min(1, gap̃ / 100, 11.5); take argmax
repeat until the wave is full; family cap by (SG, TM:RE)
Loss, precisely: the ridge minimises squared error on h; the GP hyperparameters maximise the marginal likelihood of the residuals (not a point loss, so σ is calibrated); nothing is fitted to the acquisition. Posterior uncertainty is what makes the batch diverse - no κ to tune.
Honest limits: the GP has 179 points in 19 dimensions, so it extrapolates with wide σ outside the campaign chemistry - which is exactly where Thompson sampling then spends runs. The 1574·h calibration is Gd-derived; H1 tests whether it transfers to f-in-core Nd/Sm, and the RE one-hot lets the model learn a bias if it does not.

## Slide 34
WAVES AND GENERATIONS
One packed Perlmutter job per 48 h; each wave is drawn from the pool the previous one taught
Wave 1 · global
pool = 7 sources (1,220)
TS draws 120 under the thresholds
→ 120 f-in-core relaxations
60 nodes · 4 h · ~29 h queue
Ingest
mirror → h, Ms, V per run
labels.csv (+120 rows)
H1: measured vs predicted h
GP re-fit, 10-fold CV
Wave 2 · local + global
pool = remainder
+ expand(top-25 winners)
+ new prototypes added by hand
TS draws 120 again
Ingest
labels.csv (+120)
Pareto front of (gap_RE, Ms, E_hull)
has it moved?
Wave k
same loop; pool grows by
neighbourhoods of each
wave's winners
Stop
feasible count → 0, or
front unchanged 2 waves, or
H1 fails (r < 0.5): retrain on
f-in-core rows only
What 'expand' generates from a winner
RE swap Nd ↔ Sm ↔ Pr on the same cell
Co ⅛ and ¼ of Fe, the sites nearest the RE first
early TM one Ti / V / Zr / Nb on the Fe site farthest from the RE
N into the largest RE-adjacent void (dilute and full)
each variant → MACE relax → same-model hull → descriptors → pool
What a wave returns, per cell
relaxed volume and pressure (did N / Nd fit?)
Fe / Co sublattice moments → Ms with the free-ion RE added
h = RE s+p+d polarisation → gap_RE, T*, B_RT via 1574·h
convergence flags; everything appended as a training row
no fm/ferri pair, no +U: one run is one label
Cadence: plan (minutes) → push → submit → queue 1-2 d → run 3 h → ingest (minutes). Scripts: wave_pool.py · wave_gp.py · wave_inputs.py · submit_batch.sh · sync_results.sh · wave_ingest.py, driven by wave_loop.sh; DEPLOY_NERSC.md puts the whole loop on a Perlmutter login node with scrontab.
Each wave answers a question, not just adds points: wave 1 - do the Gd-derived rules transfer to Nd/Sm (H1)? wave 2 - do the levers compose on the winners (H4)? later waves - where does the Pareto front of coupling, Ms and stability stop moving?

## Slide 35
THE PARETO FRONT, DRAWN
What 'front moved?' means: the set of hosts no other host beats on both coupling and magnetisation
How to read it
Every credible host plotted at the coupling it would give Nd (measured Gd gap scaled by (gJ−1)J) against the Ms it would give with Nd. The red line joins the hosts that are not dominated: no other host has both a larger gap and a larger Ms. Colour, where present, is the MACE hull energy of the Nd cell.
The front today
Fe₁₇Gd₂N₂ → Nd
2.04 T · 82 meV
highest Ms, below the coupling floor
BFe₁₄Gd₂ → Nd
2.03 T · 107 meV
the Nd₂Fe₁₄B reference point
Co₂Fe₇Gd₃ → Nd
1.85 T · 110 meV
RE-rich, hull +20 meV
GdFe₂ → Nd
1.81 T · 123 meV
Laves, RE-rich
Co₁₉Fe₄Gd₆ → Nd
1.59 T · 130 meV
strongest coupling at >1.5 T
CFe₁₇Gd₂ → Nd
1.35 T · 133 meV
fm side suspect, re-running
Stop rule: a wave that adds no point to this line, after its labels are measured, has not moved the front. Two such waves in a row and the pool is exhausted for the current thresholds.
Learnt: the front is the known magnets plus RE-rich cells; every point on it is either a reference compound or fails the hull or the coupling floor. The target region, upper right of both dashed lines, is empty - that is the space the waves are drawn to fill.

## Slide 36
CLOSING THE LOOP
Gaussian process for where to look, causal model for which lever, generative model for what to propose
Labelled data
180 Gd pairs → gap, h, moments, geometry
+ 20 light-RE runs
+ MACE hull for every cell
→
Gaussian process
on physics descriptors (h, Fe density,
d_RE-TM, Z_RT, Co fraction, interstitial)
→ gap, Ms, E_hull with uncertainty
→
Causal layer
structural causal model
host → S₅d → gap; interventions,
not correlations, rank the levers
→
Generative proposal
now: rule-based generators
next: diffusion conditioned on the
causal parents; MACE hull first
→
One run per cell
f-in-core relaxation gives
Ms, h → gap, T*; results
re-train every layer
every batch is a designed experiment: it must move the GP posterior or test a causal edge, not just add points
The causal model the data support
RE-TM distance
coordination
Fe / Co mix
interstitial site
S₅d on the RE
(h)
RE-TM gap
T*, anisotropy lock
Ms
(Fe density + RE)
mediator: every host lever acts through S₅d (r = 0.89); Ms is set separately by Fe density and the RE. Interventions on the left are what a generative model may propose; the dashed edge is the Co trade-off.
Gaussian process (running)
Mean = physics rules, Matern residual on h, Thompson batches sized to one packed job. Each label is one f-in-core run; a round is 120 labels per ~48 h.
Generative models (the extension)
Phase 1, now: rule-based generators - substitution, interstitials, neighbourhood of winners.
Phase 2, after wave 2-3: a conditional diffusion model (MatterGen / DOSMatGen class) fine-tuned on the pool, conditioned on the causal parents - Fe density, RE-TM distance, coordination, Co fraction, no H in the RE shell - proposing frameworks that are not decorations of known ones; MACE hull as the first filter, the GP as the second.
Phase 3: inverse design - condition on the GP posterior toward the empty region of the Pareto front; every proposal still earns its label the same way.
The campaign's product is not a compound; it is a calibrated instrument for RE-TM exchange and the first dataset a learning loop can be trained on.
Notes: GP: use h-based linear mean, Matern kernel on standardised descriptors; batch acquisition with diversity penalty sized to the packed job. Causal: DAG host-geometry -> S5d -> gap; Fe density -> Ms; interstitial site -> S5d. Generative: MatterGen-style conditioned on composition and target Fe density.